## Slide 1
Executive Statement
Lot WQ-7314 shows a localized edge-band yield loss after the September 18 ETCH-08 chamber A run.
Affected scope
Wafer WQ-7314 · route R17B · ETCH-08 / chamber A · inline metrology sample 4,812 · paired reference wafer WQ-7298.
Affected edge-band yield
91.8%
Affected vs paired-reference yield
98 → 91.8
%
Chart: Process stability and specification
| W36-1 | W36-2 | W36-3 | W36-4 | W36-5
Process stability and specification | 801.4 | 802 | 799.8 | 798.2 | 797.1
Chart: Control versus affected distribution
| Reference | Reference | Reference | Reference | Reference | Reference | Reference | Reference | Affected | Affected | Affected | Affected | Affected | Affected | Affected | Affected
Control versus affected distribution | 801.4 | 803.1 | 800.8 | 802.7 | 801.9 | 803.4 | 800.5 | 802.2 | 798 | 797.2 | 799.1 | 796.8 | 798.7 | 797.5 | 799.3 | 796.9
Verified finding
Signal · WQ-7314 edge-band yield is below the paired reference. Nine lower-right edge-band records average 91.8% versus a 98.0% paired-reference mean. Pressure shift begins after PM-44719; cause remains unconfirmed. Keep the lot contained through endpoint calibration and matched rerun. Needs verification
Corrective action
Contain WQ-7314 pending chamber requalification Do not release the lot from one correlated pressure trace. Verify endpoint calibration and a matched chamber B rerun. Contain
Affected die yield
113 observations · 0 missing · Value 91.8 to 98
N · NOTCH
MEASURED VALUE
91.8
98
Measure | Affected | Reference | Review
Edge-band yield | 91.8% | 98.0% | Contain pending matched rerun
Film thickness | 798.0 nm | 802.1 nm | Check endpoint calibration
Pressure offset | +2.4 kPa | Baseline | Association only; verify
Process Flow
Excursion signal
Compare affected
and reference
Verify chamber
mechanism
Confirm
corrective
action