## Slide 1
Executive Statement · A localized RFX-12 excursion explains the QF-8419 open-bump cluster.
Affected scope · QF-8419 · 3D-stack microbump line · RFX-12 reflow station
Screen and reference population
post-reflow electrical screen · paired lot QF-8421.
Affected microbump yield
94.26%
Affected vs paired-lot yield
98.71% → 94.26%
Chart: RFX-12 resistance subgroup sequence
| 8.12 | 8.15 | 8.08 | 8.21 | 8.18 | 8.72 | 8.81 | 8.93 | 9.02 | 8.88 | 8.76 | 8.69
RFX-12 resistance subgroup sequence
Evidence Card
Observed spatial cluster at die X 2–3 / Y 0–1
Resistance and thermal trace align after 04:20; the carrier-clean maintenance overlap remains unresolved.
Correlated
Affected and paired-lot resistance distribution
7.858
8.199
8.54
8.881
9.222
QF-8421 paired reference
QF-8419 affected lot
Diagram continues on slides 3–3
Competing mechanism · carrier-clean batch CC-392
Carrier-clean age remains a live alternative to the reflow excursion.
The 04:02 maintenance overlap could explain the elevated opens; compare the split-lot resistance profile before assigning root cause.
Unresolved · evidence conflict retained
Electrical resistance by wafer location
81 observations · 0 missing · Value 91.7 to 98.9
N · NOTCH
MEASURED VALUE
91.7
98.9
8.12
8.08
8.18
8.81
9.02
8.76
Lot / station identifier | Window | Open bumps / 1k | Evidence state
QF-8419 / RFX-12 / recipe R7C | 04:20–05:10 | 5.74 | Contained
QF-8421 / RFX-12 / recipe R7C | 05:15–06:05 | 1.29 | Paired run pending
QF-8419 / carrier clean batch CC-392 | 04:02 | 3.6 | Competing mechanism
RFX-11 / same recipe R7C | 04:20–05:10 | 1.18 | Neighbor stable

## Slide 2
Corrective action
QF-8419 containment and paired split
Owner: Device Engineering · due 2026-09-28 · preserve RFX-12 trace and carrier-clean batch CC-392.
Active

## Slide 3
Process Flow · Continued 1/1
Receive QF-8419
Verify RFX-12
trace
Run QF-8421
paired split
Release or
extend hold