## Slide 1
Body Narrative · Filtered samples retain 93.6% capacity at the final checkpoint versus 89.2% in the untreated reference. The third formulation reaches 92.1%. These samples support a limited pilot, but differences in initial conditioning and unresolved moisture results prevent a causal attribution to filtration alone.
Body Narrative
Cedar Ionics · EL-2609-C · 18 cycling checkpoints · assay lots LAB-1001 to LAB-1006 · Reliability owner · reviewed 1 October 2026. · Assay 08:20 · cycling 07:55 · duplicate result pending
Chart: Capacity retention across cycling checkpoints
| 01 · cycle 010 | 02 · cycle 020 | 03 · cycle 030 | 04 · cycle 040 | 05 · cycle 050 | 06 · cycle 060 | 07 · cycle 070 | 08 · cycle 080 | 09 · cycle 090 | 10 · cycle 100 | 11 · cycle 110 | 12 · cycle 120 | 13 · cycle 130 | 14 · cycle 140 | 15 · cycle 150 | 16 · cycle 160 | 17 · cycle 170 | 18 · cycle 180
Untreated reference | 99.4 | 98.8 | 98.2 | 97.6 | 97 | 96.4 | 95.8 | 95.2 | 94.6 | 94 | 93.4 | 92.8 | 92.2 | 91.6 | 91 | 90.4 | 89.8 | 89.2
Filtered candidate | 99.64 | 99.29 | 98.93 | 98.58 | 98.22 | 97.87 | 97.51 | 97.16 | 96.8 | 96.44 | 96.09 | 95.73 | 95.38 | 95.02 | 94.67 | 94.31 | 93.96 | 93.6
Low-salt alternative | 99.56 | 99.12 | 98.68 | 98.24 | 97.81 | 97.37 | 96.93 | 96.49 | 96.05 | 95.61 | 95.17 | 94.73 | 94.29 | 93.86 | 93.42 | 92.98 | 92.54 | 92.1
Chart: Moisture by assay batch
| LAB-1001 | LAB-1002 | LAB-1003 | LAB-1004 | LAB-1005 | LAB-1006
Moisture ppm | 17.6 | 18.2 | 19.1 | 18.4 | 18.9 | 18.7
Diagram continues on slides 2–2
Hero Title
Retention improved after filtration; the customer pilot remains conditional.
Filtered final retention
93.6%
Moisture duplicate · latest
18.7 ppm
Reference versus filtered retention
89.2% → 93.6%
Key Takeaway
Decision: release 20 pilot cells only after the moisture repeat and trace-metal duplicate pass. Keep the untreated reference running through 200 cycles and review thermal behavior before expanding.
Risk Callout
Release 20 pilot cells after duplicate assays pass
Stop release if moisture exceeds 20 ppm or copper exceeds 0.10 ppm. The assay repeat is pending; improved retention alone does not authorize shipment.
Conditional
Evidence ID | Measurement | Criterion | Owner | Disposition
REL-EL-2609-C-018 | Retention 93.6% | 94.0% target | Reliability | Pilot only
LAB-1006-MOISTURE | 18.7 ppm | 20.0 ppm max | Analytical | Duplicate pending
LAB-1006-COPPER | 0.08 ppm | 0.10 ppm max | Analytical | Verify duplicate
THERM-EL-2609-C | 34.2 C rise | 35.0 C watch | Safety | Repeat at 200 cycles
REF-EL-2609-R | 89.2% retention | Matched conditioning | Reliability | Continue reference
SHIP-PILOT-0020 | 20 cells proposed | All release checks | Operations | Hold for signatures
01 · cycle 010
06 · cycle 060
11 · cycle 110
16 · cycle 160
Untreated reference
Filtered candidate
Low-salt alternative
LAB-1001
LAB-1003
LAB-1005

## Slide 2
Release sequence · Continued 1/1
Verify moisture
duplicate
Confirm copper
result
Approve pilot
batch
Ship twenty cells
Review extended
cycling